FLAME RETARDANT POLYETHYLENE FILM

IDEALLY SUITED FOR ANY APPLICATION REQUIRING A PROTECTIVE

COVERING WITH FLAME RETARDANT CHARACTERISTICS

# TEST RESULTS*

4 MIL	6 MIL	10 MIL

BURNING CHARACTERISTICS	ASTM E 84

FLAME SPREAD INDEX		10	15	15

SMOKE DEVELOPMENT		70	75	85

TENSILE STRENGTH	ASTM D 882

MD		1700 psi	1700 psi	1700 psi

TD		1200 psi	1200 psi	1200 psi

ELONGATION	ASTM D 882

MD		225%	225%	225%

TD		350%	350%	350%

DART IMPACT	ASTM D 1709	165 g	260 g	475 g

WATER VAPOR 	ASTM E 96	.19 perm	.13 perm	.076 perm

TRANSMISSION RATE

*Meet or exceed standard specifications for Poly-America standard construction films.

### Poly-America

2000 W. Marshall Dr., Grand Prairie, TX 75051 • (972) 337-7654 • Fax (972) 337-7016